# Type: Low-E Clear Insulating Glass

***“Sungate*®*”* 400 (2) Clear + Clear** by Vitro Architectural Glass

**Outdoor Lite:** Clear (transparent) Float Glass, Sputter Coated on second surface (2)

**Indoor Lite:** Clear (transparent) Float Glass

**Low-E Coating: *“Sungate®”*** 400 (Sputtered) by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 76% | 0.32 | 0.31 | 0.60 | 0.69 | 14% |

**Approved Manufacturers:** Vitro-specific approval not required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

# Outdoor Appearance: Clear

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Tinted Insulating Glass

**Clear + *“Sungate*®” 400 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite:** Clear (transparent) Float Glass

**Indoor Lite:** Clear (transparent) Float Glass, Sputter Coated on third surface (3) **Low-E Coating: *“Sungate®”*** 400 (Sputtered) by Vitro Architectural Glass **Location:** Third Surface (3)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 76% | 0.32 | 0.31 | 0.63 | 0.73 | 14% |

**Approved Manufacturers:** Vitro-specific approval not required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

# Outdoor Appearance: Clear

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Clear Insulating Glass

***“Sungate*®*”* 400 (2) *“Starphire*®*”* + *“Starphire®”*** by Vitro Architectural Glass

**Outdoor Lite: *“Starphire®”*** (low-iron [a specially formulated glass type to eliminate the green hue commonly associated with clear glass]) Float Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

**Indoor Lite: *“Starphire®”*** (low-iron) Float Glass

**Low-E Coating: *“Sungate®”*** 400 (Sputtered) by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 80% | 0.32 | 0.31 | 0.68 | 0.78 | 14% |

**Approved Manufacturers:** Vitro-specific approval not required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

# Outdoor Appearance: Clear

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Tinted Insulating Glass

***“Solexia*®*”* + *“Sungate*®*”* 400 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Solexia®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass, Sputter Coated on third surface (3) **Low-E Coating: *“Sungate®”*** 400 (Sputtered) by Vitro Architectural Glass **Location:** Third Surface (3)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 66% | 0.32 | 0.31 | 0.44 | 0.50 | 11% |

**Approved Manufacturers:** Vitro-specific approval not required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Light-green

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Tinted Insulating Glass

***“Atlantica*®*”*** + ***“Sungate*®*”* 400 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Atlantica®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass, Sputter Coated on third surface (3) **Low-E Coating: *“Sungate®”*** 400 (Sputtered) by Vitro Architectural Glass **Location:** Third Surface (3)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 58% | 0.32 | 0.31 | 0.35 | 0.40 | 9% |

**Approved Manufacturers:** Vitro-specific approval not required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Emerald-green

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Tinted Insulating Glass

***“Azuria*®*”* + *“Sungate*®*”* 400 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Azuria®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass Sputter Coated on third surface (3) **Low-E Coating: *“Sungate®”*** 400 (Sputtered) by Vitro Architectural Glass **Location:** Third Surface (3)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 59% | 0.32 | 0.31 | 0.34 | 0.39 | 10% |

**Approved Manufacturers:** Vitro-specific approval not required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Aqua-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Tinted Insulating Glass

***“Solarbronze*®*”* + *“Sungate*®*”* 400 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Solarbronze®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass Sputter Coated on third surface (3) **Low-E Coating: *“Sungate®”*** 400 (Sputtered) by Vitro Architectural Glass **Location:** Third Surface (3)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 46% | 0.32 | 0.31 | 0.44 | 0.50 | 8% |

**Approved Manufacturers:** Vitro-specific approval not required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Warm-bronze

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Tinted Insulating Glass

***“Solargray*®*”* + *“Sungate*®*”* 400 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Solargray®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass Sputter Coated on third surface (3) **Low-E Coating: *“Sungate®”*** 400 (Sputtered) by Vitro Architectural Glass **Location:** Third Surface (3)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 38% | 0.32 | 0.31 | 0.39 | 0.44 | 7% |

**Approved Manufacturers:** Vitro-specific approval not required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Cool light-gray

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Reflective Tinted Low-E Insulating Glass

***“Graylite*®*”* II + *“Sungate*®*”* 400 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Graylite®”*** II Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass Sputter Coated on third surface (3) **Low-E Coating: *“Sungate®”*** 400 (Sputtered) by Vitro Architectural Glass **Location:** Third Surface (3)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 8% | 0.32 | 0.31 | 0.15 | 0.17 | 4% |

**Approved Manufacturers:** Vitro-specific approval not required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Dark-gray

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Tinted Insulating Glass

***“Solarblue*®*”* + *“Sungate*®*”* 400 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Solarblue®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass Sputter Coated on third surface (3) **Low-E Coating: *“Sungate®”*** 400 (Sputtered) by Vitro Architectural Glass **Location:** Third Surface (3)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 48% | 0.32 | 0.31 | 0.42 | 0.49 | 8% |

**Approved Manufacturers:** Vitro-specific approval not required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Light sky-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Tinted Insulating Glass

***“Pacifica*®*”* +*“Sungate*®*”* 400 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Pacifica®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass Sputter Coated on third surface (3) **Low-E Coating: *“Sungate®”*** 400 (Sputtered) by Vitro Architectural Glass **Location:** Third Surface (3)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 37% | 0.32 | 0.31 | 0.30 | 0.34 | 7% |

**Approved Manufacturers:** Vitro-specific approval not required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Deep-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Tinted Insulating Glass

***“Optigray*®*”* + *“Sungate*®*”* 400 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Optigray®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass Sputter Coated on third surface (3) **Low-E Coating: *“Sungate®”*** 400 (Sputtered) by Vitro Architectural Glass **Location:** Third Surface (3)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 54% | 0.32 | 0.31 | 0.46 | 0.52 | 9% |

**Approved Manufacturers:** Vitro-specific approval not required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Ultra-neutral, light-gray

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass