# Type: Uncoated Tinted Insulating Glass

***“Azuria*®*”* + Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Azuria®”*** Float Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass

**Tint Color: *“Azuria®”*** by Vitro Architectural Glass

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 61% | 0.47 | 0.50 | 0.39 | 0.45 | 11% |

**Approved Manufacturers:** Vitro-specific approval not required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Aqua-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Tinted Insulating Glass

***“Azuria*®*”* + *“Sungate*®*”* 400 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Azuria®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass Sputter Coated on third surface (3) **Low-E Coating: *“Sungate®”*** 400 (Sputtered) by Vitro Architectural Glass **Location:** Third Surface (3)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 59% | 0.32 | 0.31 | 0.34 | 0.39 | 10% |

**Approved Manufacturers:** Vitro-specific approval not required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Aqua-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

***“Solarban*®*”* 60 (2) *“Azuria*®*”* + Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Azuria®”*** Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

**Indoor Lite:** Clear (transparent) Float Glass

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 54% | 0.29 | 0.27 | 0.28 | 0.32 | 8% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Aqua-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

***“Azuria*®*”* + *“Solarban*®*”* 60 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Azuria®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass, Sputter Coated on third surface (3)

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Third Surface (3)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 54% | 0.29 | 0.27 | 0.31 | 0.36 | 9% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Aqua-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

**Type: Solar Control Low-E Tinted Insulating Glass**

***“Solarban*®*”* 67 (2) *“Azuria*®*”* + Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Azuria®”*** Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

**Indoor Lite:** Clear (transparent) Float Glass

**Low-E Coating: *“Solarban®”*** 67 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 42% | 0.29 | 0.27 | 0.23 | 0.26 | 13% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Aqua-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

***“Azuria*®*”* + *“Solarban*®*”* 67 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Azuria®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass, Sputter Coated on third surface (3)

**Low-E Coating: *“Solarban®”*** 67 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Third Surface (3)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 42% | 0.29 | 0.27 | 0.29 | 0.33 | 11% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Aqua-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Clear Insulating Glass

***“Solarban*®*”* 70 (2) *“Azuria*®*”* + Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Azuria®”*** Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

**Indoor Lite:** Clear (transparent) Float Glass

**Low-E Coating: *“Solarban®”*** 70 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 50% | 0.28 | 0.26 | 0.24 | 0.27 | 10% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Aqua-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

***“Azuria*®*”* + *“Solarban*®*”* 70 (3) †** by Vitro Architectural Glass

**Outdoor Lite: *“Azuria®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Float Glass by Vitro Architectural Glass, Sputter Coated on third surface (3) **†**

**Low-E Coating: *“Solarban®”*** 70 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Third Surface (3)

**† *Solarban®*** 70 for annealed applications is applied to ***Acuity™*** glass; heat-treated applications will require either clear or ***Acuity™*** glass depending on manufacturing process.

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 49% | 0.28 | 0.26 | 0.29 | 0.33 | 9% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Aqua-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Tinted Reflective Insulating Glass

***“Solarban*®*”* 90 (2) *“Azuria*®*”* + Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Azuria®”*** Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

**Indoor Lite:** Clear (transparent) Float Glass

**Low-E Coating: *“Solarban®”*** 90 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 39% | 0.29 | 0.27 | 0.21 | 0.24 | 9% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Aqua-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Solar Control Low-E Tinted Insulating Glass

***“Azuria*®*”* + *“Solarban*®*”* 90 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Azuria®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass, Sputter Coated on third surface (3)

**Low-E Coating: *“Solarban®”*** 90 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Third Surface (3)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 39% | 0.29 | 0.27 | 0.27 | 0.31 | 13% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Aqua-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Low-E Tinted Reflective Insulating Glass

***“Solarban*®*”* R100 (2) *“Azuria*®*”* + Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Azuria®”*** Glass by Vitro Architectural Glass, Sputter Coated on second surface (2)

**Indoor Lite:** Clear (transparent) Float Glass

**Low-E Coating: *“Solarban®”*** R100 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 32% | 0.29 | 0.27 | 0.19 | 0.22 | 21% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Aqua-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Subtly Reflective Tinted Insulating Glass

***“Vistacool*®*”* (2) *“Azuria*®*”* + Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Vistacool®* (2) *Azuria®”*** Glass by Vitro Architectural Glass

**Tint Color: *“Azuria®”*** by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass

**Reflective Coating: *“Vistacool®”*** by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 47% | 0.47 | 0.50 | 0.34 | 0.39 | 21% |

**Approved Manufacturers:** Vitro-specific approval not required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Subtly reflective aqua-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Reflective Tinted Insulating Glass

***“Solarcool*®*”* (2) *“Azuria*®*”* + Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Solarcool®* (2) *Azuria®”*** Glass by Vitro Architectural Glass

**Tint Color: *“Azuria®”*** by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass

**Reflective Coating: *“Solarcool®”*** by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 24% | 0.47 | 0.50 | 0.25 | 0.29 | 20% |

**Approved Manufacturers:** Vitro-specific approval not required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Reflective aqua blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Reflective Tinted Solar Control Low-E Insulating Glass

***“Vistacool*®*”* (2) *“Azuria*®*”* + *“Solarban*®*”* 60 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Azuria®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass, Sputter Coated on third surface (3)

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass **Location:** Third Surface (3)

**Reflective Coating: *“Vistacool®”*** by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 42% | 0.29 | 0.27 | 0.26 | 0.30 | 20% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Subtly reflective aqua-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Reflective Tinted Solar Control Low-E Insulating Glass

***“Vistacool*®*”* (2) *“Azuria*®*”* + *“Solarban*®*”* 90 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Azuria®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass, Sputter Coated on third surface (3)

**Low-E Coating: *“Solarban®”*** 90 Solar Control (Sputtered) by Vitro Architectural Glass **Location:** Third Surface (3)

**Reflective Coating: *“Vistacool®”*** by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 31% | 0.29 | 0.27 | 0.23 | 0.26 | 23% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Subtly reflective aqua-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Subtly Reflective Solar Control Low-E Insulating Glass

***“Vistacool*®*”* (2) *“Azuria*®*”* + *“Solarban*®*”* 70 (3) †** by Vitro Architectural Glass

**Outdoor Lite: *“Azuria®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Float Glass by Vitro Architectural Glass, Sputter Coated on third surface (3) †

**Low-E Coating: *“Solarban®”*** 70 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Third Surface (3)

**Reflective Coating: *“Vistacool®”*** by Vitro Architectural Glass

**Location:** Second Surface (2)

**† *Solarban®*** 70 for annealed applications is applied to ***Acuity™*** glass; heat-treated applications will require either clear or ***Acuity™*** glass depending on manufacturing process.

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 38% | 0.28 | 0.26 | 0.24 | 0.28 | 21% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Subtly reflective aqua-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Reflective Tinted Solar Control Low-E Insulating Glass

***Solarcool*®*”* (2) *“Azuria*®*”* + *“Solarban*®*”* 60 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Azuria®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass, Sputter Coated on third surface (3)

**Low-E Coating: *“Solarban®”*** 60 Solar Control (Sputtered) by Vitro Architectural Glass **Location:** Third Surface (3)

**Reflective Coating: *“Solarcool®”*** by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 21% | 0.29 | 0.27 | 0.17 | 0.19 | 19% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Reflective aqua blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Reflective Solar Control Low-E Insulating Glass

***“Solarcool*®*”* (2) *“Azuria*®*”* + *“Solarban*®*”* 70 (3) †** by Vitro Architectural Glass

**Outdoor Lite: *“Azuria®”*** Glass by PPG Industries, Inc.

**Indoor Lite:** Float Glass by Vitro Architectural Glass, Sputter Coated on third surface (3)†

**Low-E Coating: *“Solarban®”*** 70 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Third Surface (3)

**Reflective Coating: *“Solarcool®”*** by Vitro Architectural Glass

**Location:** Second Surface (2)

**† *Solarban®*** 70 for annealed applications is applied to ***Acuity™*** glass; heat-treated applications will require either clear or ***Acuity™*** glass depending on manufacturing process.

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 19% | 0.28 | 0.26 | 0.16 | 0.18 | 19% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Reflective aqua blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Reflective Tinted Solar Control Low-E Insulating Glass

***“Solarcool*®*”* (2) *“Azuria*®*”* + *“Solarban*®*”* 90 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Azuria®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass, Sputter Coated on third surface (3)

**Low-E Coating: *“Solarban®”*** 90 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Third Surface (3)

**Reflective Coating: *“Solarcool®”*** by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 16% | 0.29 | 0.27 | 0.15 | 0.17 | 20% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product

Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Reflective aqua blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Reflective Tinted Solar Control Low-E Insulating Glass

***“Solarcool*®*”* (1) *“Azuria*®*”* + *“Solarban*®*”* 90 (3) Clear** by Vitro Architectural Glass

**Outdoor Lite: *“Azuria®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass, Sputter Coated on third surface (3)

**Low-E Coating: *“Solarban®”*** 90 Solar Control (Sputtered) by Vitro Architectural Glass

**Location:** Third Surface (3)

**Reflective Coating: *“Solarcool®”*** by Vitro Architectural Glass

**Location:** Second Surface (2)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 15% | 0.29 | 0.27 | 0.13 | 0.15 | 37% |

**Approved Manufacturers:** Vitro Certified™ Fabricator Required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Reflective aqua blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass

# Type: Reflective Tinted Insulating Glass

***“Solarcool*®*”* (1) *“Azuria*®*”* + Clear**

**Outdoor Lite: *“Azuria®”*** Glass by Vitro Architectural Glass

**Indoor Lite:** Clear (transparent) Float Glass

**Reflective Coating: *“Solarcool®”*** by Vitro Architectural Glass

**Location:** First Surface (1)

# Performance Values

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Visible Light Transmittance | U-Value Winter | U-Value Summer | SHGC | Shading Coefficient | Outdoor Visible Light Reflectance |
| 23% | 0.47 | 0.50 | 0.22 | 0.25 | 37% |

**Approved Manufacturers:** Vitro-specific approval not required

**Certification:** Both lites to be Cradle to Cradle Certified™, minimum Bronze Level, by Cradle to Cradle Product Innovation [Institute (www.c2ccertified.org](http://www.c2ccertified.org/)).

**Outdoor Appearance:** Reflective aqua-blue

**Insulating Unit Construction:** 1/4” (6mm) glass + 1/2” (13mm) air space + 1/4” (6mm) glass